## Slide 1: Short-range order in hydrogen diffusion of FCC materials
Gavin DeBrun, Youfu Qian, Daegun You

## Slide 2: Motivation
Hydrogen diffusion into metals and alloys can cause embrittlement and result in cracking
Fundamental understanding of hydrogen diffusion is needed
Adrián Del-Pozo et al., Current Trends and Future Developments on (Bio-) Membranes, 2020, 139-168
D. Lee, J. J. Vlassak, K. Zhao, ACS Applied Materials & interfaces 8, 10995-11000 (2016)
Order of atomic configuration in alloys
A99B1
A50B50
Solute concentration of alloys
…
Nature 602, 437-441 (2022)

## Slide 3: Short-range order
Warren-Cowley SRO parameter
Simple way to characterize short-range order (SRO) of alloys
1st NN shell
2nd NN shell
3rd NN shell
Consider different nearest neighbor (NN) atoms
J. M. Cowley, Physical Review 120, 1648-1657, 1960
N. Norman, B. E. Warren. Journal of Applied Physics 22, 483-486, 2004
Cu
Al
, random
, cluster (same types)
, order (different types)
Average for overall supercell

## Slide 4: Interatomic potential
Lennard-Jones (LJ) potential
Lorentz-Berthelot combination rule
Benchmark of LJ potential parameters on determination of lattice constants in angstrom (Å) for example metals**
*N. Hu, X. Sun, and A. Hsu, The Journal of chemical physics, 123, 4, 2005.
**W. P. Davey, Physical Review, 25, 6, 753, 1925.
 | ε0 [eV] | σ [Å] | A [eV/Å12] | B [eV/Å6]
Cu | 0.2047 | 2.616 | 21023 | 131.2
Al | 0.1743 | 2.925 | 68384 | 218.3
H | 0.0016 | 2.460 | 309.7 | 1.397
Literature data of the LJ potential for the simulation elements**
 | In this work | Experiment
Cu | 3.646 Å | 3.61 Å
Al | 4.079 Å | 4.05 Å

## Slide 5: Implementation

## Slide 6: Monte Carlo swapping atomic species
Construction of different SRO configuration of alloys
Initial random configuration
Randomly swap between Cu and Al atom
LJ-based energy calculation
Accept the configuration
Save data
Reject the configuration
Recall the previous one
: Temperature scaling factor
: random number in
Metropolis criterion
ex) 1 Cu <-> 1 Al
Selected 3 configurations
Cu80Al20
Random
Intermediate
Final

## Slide 7: MD Relaxation
  We equilibrate the selected atomic structures from the MC swapping without hydrogen
  Then add hydrogen to interstitial site and equilibrate again
Optimized Lattice Parameters:
LJ-based MD relaxation of FCC structure
 | In this work
Cu80Al20 | 3.764 Å
Cu60Al40 | 3.863 Å
Lattice
Octahedral (Octa)
Tetrahedral (Tetra)
Cu
Al
H
FCC interstitial sites:

## Slide 8: MD Hydrogen Stepping
Initial configuration from MD relaxation

## Slide 9: Results

## Slide 10: Molecular dynamics simulation
Formation energy (Ef) due to local SRO effect of hydrogen () and overall SRO of supercell () in FCC alloys
(= -3.38 eV)
: total energy of the relaxed supercell of target material “with hydrogen”
: total energy of the relaxed supercell of target material “without hydrogen”
: energy of a hydrogen molecule
D. You et al., Scripta Materialia 183 (2020) 1–5
X. L. Ren et al., Acta Materialia 180 (2019) 189-198
Local SRO of hydrogen
Overall SRO of supercell ()

## Slide 11: Diffusion of hydrogen
a
b
c
Cu
Al
H
Diffusion pathways are estimated by the formation energy in different interstitial sites
Local SRO of hydrogen is correspondingly recorded

## Slide 12: Diffusion of hydrogen
Effect of Al solute concentration and temperature in formation energy upon diffusion
Cu80Al20
Thermally assisted
No ordering effect

## Slide 13: Conclusion and Limitations
Electron and charge fields of atoms
LJ potential with Lorentz-Berthelot rule
Neglect supercell size effect
MC swapping of atomic species development
Stability of hydrogen interstitial with both local and bulk SRO effect
Estimation of diffusion pathways of hydrogen in FCC metals and alloys
SRO, temperature, and solute concentration effects for hydrogen diffusion
Local SRO of hydrogen

## Slide 14: Questions?